## Slide 1: High Pressure Heat Treatment - Phase Transformation Under Isostatic Pressure in HIP
Magnus Ahlfors
Applications engineer Isostatic pressing
magnus.ahlfors@quintusteam.com

## Slide 2: Project
Joint member project within the Powder Metallurgy Member Research Consortia at Swerea KIMAB, Sweden
Participating companies:
  Quintus Technologies AB Magnus Ahlfors, Stefan Sehlstedt
  AB Sandvik Materials Technology Linn Larsson, Martin Östlund
  Höganäs AB Dimitris Chasoglou

## Slide 3: Outline
Purpose and aim
Background
Experiments
Results
Discussion and conclusions

## Slide 4: Purpose and aim
Purpose: Rapid quench HIP furnaces enables heat treatment in the HIP
  Heat treatment and quenching performed under high external pressure
  Very little data on thermodynamics under pressure found in literature e.g. TTT, CCT etc.
  Is conventional heat treat recipes transferable to HIP:ing?
Aim: Investigate whether a typical HIP pressure of 1700 bar is enough to shift the austenite to pearlite phase transformation towards longer times and quantify the effect

## Slide 5: Background
Studies form 1960s-70s on the influance of extreme pressures on phase transformation kinteics in Fe-C system
  Nilan, Hilliard, Radcliff, Fujita
  Theory on reduction of transformation
    Lower carbon diffusivity at elevated pressures
A. Weddeling has used URQ HIP to study the influence of high pressure quenching on microstructure
  Results suggest that the bainite formed during quenching under HIP pressure is not only formed later in time but also at lower temperatures
  Densifying and Hardening of Martensitic Steel Powders in HIP Units Providing High Cooling Rates, EuroPM2015

## Slide 6: Materials selection
4340 (SS2541)
  A wellknown quench and temper steel
  Data existing in litterature
  Sufficient time to perlite start
Chemical composition
Elements [%] | C | Mn | Si | Cr | Ni | Mo | Cu | Fe
4340 | 0.37 | 0.74 | 0.26 | 1.45 | 1.50 | 0.19 | 0.16 | bal.

## Slide 7: Experimental procedure and parameter selection
TTT diagram experimental approach for a high and a low pressure
  Austenize at 850 °C for >20 minutes
  Rapid quench to 650°C (park in front of the perlite nose)
  Five different hold times (1000s, 1500s, 2000s, 3000s, 6000s)
  One low and one high pressure (100 and 1700 bar)
    1700 bar = maxiumum possible pressure
    100 bar = minimum possible pressure
  Microstructure analysis and hardness measurment
Schematic of test procedure

## Slide 8: Experimental procedure
Test set-up:
  Cylindrical rod specimens: 25 x 25 mm (1” x 1”)
  Drilled hole to center of specimen
  Thermocouples in gas in hot zone
  Thermocouple in center of specimen
Test speciemen
Thermocouples
Set-up in HIP furnace

## Slide 9: Results from HIP cycles
HIP log curve for 3000 s, 1700 bar
Perlite transformation
- Exoterm reaction
HIP log curve for 3000 s, 100 bar

## Slide 10: Results of microscopy and hardness measurements
1500 sec isotherm @100 bar
19 % pearlite
Hardness: 536 HV
1500 sec isotherm @1700 bar
10 % pearlite
Hardness: 572 HV
Pearlite
Martensite
Pearlite
Martensite

## Slide 11: Results of microscopy and hardness measurements
2000 sec isotherm @100 bar
70 % pearlite
Hardness: 344 HV
2000 sec isotherm @1700 bar
26 % pearlite
Hardness: 497 HV
Pearlite
Martensite
Pearlite
Martensite

## Slide 12: Microscopy and hardness summary
1000 seconds is too short hold time
  Virtually 0 % perlite and similar hardness for both pressures
3000 and 6000 seconds are too long hold times
  Virtually 100 % perlite and similar hardness for both pressures

## Slide 13: Conclusions
All phase fraction evaluation results indicate that HIP pressure pushes austenite – pearlite transformation towards longer times
All hardness measurement results indicate that HIP pressure pushes austenite – pearlite transformation towards longer times
100 and 1700 bar compared, not atmospheric pressure!

## Slide 14: Benefits
  Automatically increased hardenability when quenching under pressure
  Possibility to:
    Use less alloying elements
    Quench thicker sections
    Use slower cooling for the same hardening response

## Slide 15: High pressure heat treatment – unexplored field
CCT and TTT diagrams, heat treatment recipes etc.
  all for atmospheric pressure
Only Fe-C system investigated in this study
What is the pressure influence on other common materials?
  Al, Ti, Ni-base, CoCr etc.
What other effects can pressure have on conventional heat treatment?
Unexplored and interesting field where research is needed!

## Slide 16
Thank you for your attention!
Magnus Ahlfors
Applications Engineer
Magnus.Ahlfors@quintusteam.com