## Slide 1: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Controlled uniform load cooling in production scale HIP equipment
Maxime Pauwels, Engineered Pressure Systems International NV
HIP’17 Sydney – Australia
7/12/2017

## Slide 2: EPSI – The company – US & EU
EPSI Incorporated
Haverhill
MA, USA
EPSI International
Temse
Belgium
Engineered Pressure Systems International N.V.
Saar Pulvermetall
Saarwellingen
Germany

## Slide 3: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
HIP140-850*2500M
Useful inner dimensions: 850 mm diameter and 2500mm length
6 separate radial heating zone
Pressure up to 140 MPa

## Slide 4: EPSI – The company – US &EU
Engineered Pressure Systems International N.V.
10 loading elements can also be used to steer the HIP
Heating zone 1
Control thermo element
Redundant element
Heating zone 3
Heating zone 4
Heating zone 5
Heating zone 6
Bottom heating
2 Bottom heating elements with control thermo element and redundant element
Heating zone 2
Control thermo element
Redundant element
Control thermo element
Redundant element
Control thermo element
Redundant element
Control thermo element
Redundant element
Control thermo element
Redundant element
Thermal build up

## Slide 5: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Natural cooling
Temperature difference of +-120 °C possible!

## Slide 6: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Rapid cooling
Cooling speed augmented
BUT large temperature differences!

## Slide 7: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Jet cooling

## Slide 8: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Controlled cooling 1

## Slide 9: EPSI – The company – US & EU
Engineered Pressure Systems International N.V.
Controlled cooling 2

## Slide 10
Engineered Pressure Systems International N.V.
416 K in 9‘ = 46 K/Minute
1216°C
800°C
1216 °C +/- 6°C
Temperature accuracy during jet cooling +- 6 °C
With all TCs
Jet cooling results with 2800 kg load

## Slide 11
Engineered Pressure Systems International N.V.
Heating and cooling – energy calculation

## Slide 12
Engineered Pressure Systems International N.V.
Many thanks for your attention