## Slide 1: Wear of PM HIP metal matrix composites – influence of carbide type
Notes: Sandvik är en högteknologisk verkstadskoncern med avancerade produkter och en världsledande position inom utvalda områden.

## Slide 2: Wear of PM HIP metal matrix composites – influence of carbide type
Tomas Berglund Josefin Hall
Technical Marketing Researcher Sandvik Powder Solutions Dalarna University

## Slide 3: Presentation Outline
Introduction
  Applications
  Materials
Experimental
  Material and manufacturing
  Tribological testing
Results
  Microstructure
  Tribological characteristics
  Field tested components
Conclusions

## Slide 4: Introduction
Composed of a ductile matrix and hard particles to improve wear resistance
MMCs containing tungsten carbide are often used as overlays in the mining industry
HIP-cladding is an attractive alternative to e.g. laser cladding, HVOF and PTAW overlays
Several forms of tungsten carbide is in the overlays
Properties are primarily controlled by:
  Carbide type
  Matrix composition
  Carbide size and amount
  Consolidation parameters
Wear resistant metal matrix composites

## Slide 5: Presentation Outline
Introduction
  Applications
  Materials
Experimental
  Material and manufacturing
  Tribological testing
Results
  Microstructure
  Tribological characteristics
  Field tested components
Conclusions

## Slide 6: Experimental
Consolidated at 1150ºC, 1000bar for 2 hours
All materials have the same Ni-base matrix alloy
The same powder sizes are used for all materials.
50 vol.% of tungsten carbide
  Fused crushed carbide (W2C/WC), F50
  Fused spherical carbide (W2C/WC), FSP50
  Macrocrystaline WC, MC50
Materials

## Slide 7: Experimental
Abrasion testing
  Low stress abrasion testing, dry sand rubber wheel (ASTM G65)
  High stress abrasion testing, wet sand steel wheel (ASTM B611)
Scratch testing
  Quartz stylus
  Testing was performed to study carbide damage during abrasion
Hardness testing
  Macro, matrix, carbide
Field tested parts
Material testing
 | Low stress | High stress
Base procedure | ASTM G65 A mod. | ASTM B611
Abrasive media | Silica sand #50-70 | 30# Al2O3
HV abrasive | 1100 HV | 2200 HV
Slurry | N/A | 80% abrasive 20% H20
Wheel material | Rubber | AISI 1020 Steel
Wheel RPM | 212 | 100±5 rpm
Sand flow rate | 375 g/min | 
Force | 130N | 200 N
No revolutions | 6000 | 1000
Sliding distance | 4309 meters | 518-530 meter

## Slide 8: Presentation Outline
Introduction
  Applications
  Materials
Experimental
  Material and manufacturing
  Tribological testing
Results
  Microstructure
  Tribological characteristics
  Field tested components
Conclusions

## Slide 9: Results
F50 has the highest degree of carbide dissolution followed by FSP50 and MC50
The fused carbides have no to little cracking
The MC carbides have a significant amount of cracking
For all material there are a small amount of secondary phases in the matrix between the primary carbides
Microstructure

## Slide 10: Results
Macro hardness of MC50 is slightly lower compared to the F50 and FSP50
The fused spherical carbide is the hardest followed by fused crushed and macrocrystalline
The matrix in F50 has the highest hardness
  Carbide dissolution increases alloying content of matrix
  Solid solution strengthening by W as well as carbide precipitation
Hardness
Figure . Macro hardness of material and micro hardness of carbides and matrix.

## Slide 11: Results
Low stress abrasion is often done in 1 or 2 passes (ASTM G65)
Wear doesn’t stabilize until pass 4 to 6
  Just matrix being worn away in the first passes
Initially the wear resistance of F50 is lower and MC50 higher
  Carbide dissolution increases mean free path
After pass 4 the performance of the material is similar.
Even after 6 passes the majority of the wear is in the matrix between carbides
Low stress abrasion testing

## Slide 12: Results
Low stress abrasion is often done in 1 or 2 passes (ASTM G65)
Wear doesn’t stabilize until pass 4 to 6
  Just matrix being worn away in the first passes
Initially the wear resistance of F50 is lower and MC50 higher
  Carbide dissolution increases mean free path
After pass 4 the performance of the material is similar.
Even after 6 passes the majority of the wear is in the matrix between carbides
Low stress abrasion testing

## Slide 13: Results
Low stress abrasion is often done in 1 or 2 passes (ASTM G65)
Wear doesn’t stabilize until pass 4 to 6
  Just matrix being worn away in the first passes
Initially the wear resistance of F50 is lower and MC50 higher
  Carbide dissolution increases mean free path
After pass 4 the performance of the material is similar.
Even after 6 passes the majority of the wear is in the matrix between carbides
Low stress abrasion testing

## Slide 14: Results
Much higher wear compared to low stress abrasion testing
MC50 performs significantly worse than the other two materials
  Lower hardness carbide
Significant higher amount of carbide damage in MC50
High stress abrasion testing
Chart: Volume loss [cm3]
| F50 | MC50 | FSP50
Vol. loss B611 | 0.14672 | 0.25042 | 0.13367

## Slide 15: Results
The fused carbide show very little signs of bulk cracking
Damage to the fused carbide is predominantly at the edges in or close to the dissolved region
The macrocrystalline carbide displays a tendency to bulk cracking
  Also indicated in hardness testing
Scratch testing

## Slide 16: Results
Large similarities to low stress abrasive wear
  Slurry flowing over the surface
Matrix worn away between carbide
Rounded carbides indicates mild wear
Some carbide damage
  Cracking, micro chipping and abrasion
Field tested part - Slurry

## Slide 17: Results
Similarities to high stress abrasion but more carbide damage
Surface topography is relatively flat compared to pump part
  Carbide damage and abrasion
Embedded particles in the surface
Field tested part - Crushing

## Slide 18: Presentation Outline
Introduction
  Applications
  Materials
Experimental
  Material and manufacturing
  Tribological testing
Results
  Microstructure
  Tribological characteristics
  Field tested components
Conclusions

## Slide 19: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 20: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 21: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 22: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 23: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 24: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is similar to low stress abrasion
The wear mechanism in the crusher part is more towards high stress abrasion

## Slide 25: Summary and Conclusions
Angular fused tungsten carbide exhibit a higher degree of carbide dissolution compared to spherical fused carbide when HIPed at the same conditions
Macrocrystalline carbide exhibits significantly lower degree of carbide dissolution compared to the fused carbides
Lower carbide dissolution result in better wear resistance in the early stages of wear during low stress abrasion testing using silica sand
There is a good correlation between carbide hardness and wear resistance in high stress abrasion testing using Al2O3 particles
Higher degree of carbide dissolution increases the hardness of the matrix
The wear mechanism in the slurry part is more similar to low stress abrasion
The wear mechanism in the crusher part is similar to high stress abrasion

## Slide 26: Thank You for Your attention!
Tomas Berglund Sandvik Powder Solutions AB Sandvik Materials Technology Phone: +46 26 65408 Mailto:tomas.berglund@sandvik.com
Josefin Hall Researcher Dalarna University Mailto: joh@du.se